Coloring Your Woodturnings

Duane Hill

Jan 2011

Coloring in General

- Coloring can take many forms

- Staining

- Stains are made up a larger particles and essentially stay on the surface or slight penetration of the wood

- Dyeing

- Dyes are made up of small particles that totally dissolve in their solvent; thereby getting much deeper penetration

- Dye solvents are typically water or denatured alcohol

- Aniline dyes may be dissolved in water or alcohol, check specific dye for dissolving agent

- Inks are considered dyes

- India ink makes a great black

- Leather  dyes also work well

- Painting

- Larger particles, stays on surface

- Can be opaque or transparent

- Transparent lets grain show through

- Markers

- Typically alcohol based

- Prismacolor

- Craft Supplies

- Sharpies

- Pam uses these for coloring her pieces

- Make sure the form is perfect and the surface has no flaws; coloring will bring out the flaws

- Additional materials

- Gloves

- Smock for clothes

- Glass jars

- Eye droppers

- Color wheel

- Pallet

- Paper towels

- Air compressor for air brushing

- Air brush

Masking

- Good for limiting where dye/paint goes

- Masking fluids

- Latex

- Stuff like rubber cement

- Sign mask

- Can be sprayed on or brushed on

- Best for non-consistent diameters

- Frisket

- Could for consistent diameters

- Can be cut with Xacto knife

- Woodburning makes an effective and decorative mask

Dyeing

- Preparation

- Sanding

- Sand to no finer that 320 grit

- Much finer and the ends of the wood fibers get burnished over and the dye won’t penetrate

- Seal the surface with thinned shellac

- Option, depending on wood and thickness

- Seal inside surface to greatly reduce bleed through

- Seal both surfaces (inside and out) for best bleed through protection

- Seal top surface if using a mask

- Lightly sand after sealing (320 grit)

- Apply first layer of dye

- Apply darker colors first

- Can be brushed on or dabbed on with paper towel

- Allow it to dry

- Lightly sand with 320 grit.

- Can sand through in areas, if desired

- Apply other dye layers

- Can cover all or in spots

- Sand with 320 grit

- Remove masking

- Sand to 400 and finer grits

- Apply finish

- I like to use an oil finish for first two or three coats and then add a poly as a top coat

- Other Notes

- Use blue as a first dye color if dyeing black

- Without blue, the black takes on a bronze cast

- Can dilute dye with either alcohol or water

- Final coat is a “wash”, highly diluted dye

- Can mix colors

- Use eye dropper to retrieve dye

- One dropper per color

- Count drops of each dye and record

- Use pallet or glass jar to mix in

Painting

- Preparation

- Sand to final grit

- Define paint area

- Carve

- Woodburn

- Masking

- Apply paint

- Brush

- Air brush

- Final sanding

- Apply finish

Markers

- Preparation

- Sand to final grit

- Outline areas to be colored with woodburning

- Color areas with markers

- Apply fixative

- Avoid alcohol finishes

- Apply finish